## Slide 1: Progress on DRDC projects
Yutong Zhao
Dec 3rd 2018

## Slide 2
Empty holder
Icing sugar
KClO3
KNO3
NaCl
NaNO3
NH4NO3
NH4NO3& KNO3
Mixture
Empty holder
KClO3
KNO3
NaCl
Icing sugar
NaNO3
NH4NO3
NH4NO3& KNO3
Mixture
Optical image
Microwave image

## Slide 3
Materials | Sample mass(mg) | Density | Volume fraction | Permittivity() |  | -(MHz)
Air | 0 | ~ 0 | 100% | ~1 | 1 | 1.001
KClO3 | 79 | 2.32 g/cm3 | 38.01% | 4.36 | 2.28 | 0.852
KNO3 | 84 | 2.109 g/cm3 | 44.27% | 3.91 | 2.28 | 0.618
NaCl | 102 | 2.17 g/cm3 | 52.03% | 4.71 | 2.95 | 0.485
NaNO3 | 95 | 2.257 g/cm3 | 36.59% | 4.60 | 2.69 | 0.418
NH4NO3 | 56 | 1.72 g/cm3 | 47.06% | 5.37 | 2.56 | 0.458
Icing sugar | 49 | 0.65 g/cm3 | 84.27% | 1.90 | 1.76 | 0.820
NH4NO3 & KNO3 Mixture | 68 | 1.94 g/cm3 | 38.89% | 4.63 | 2.41 | 0.472
Materials | Sample mass(mg) | Density | Volume fraction |  |  | 
Air | 0 | ~ 0 | 100% | ~1 | 1 | 1.001
KClO3 | 79 | 2.32 g/cm3 | 38.01% | 4.36 | 2.28 | 0.852
KNO3 | 84 | 2.109 g/cm3 | 44.27% | 3.91 | 2.28 | 0.618
NaCl | 102 | 2.17 g/cm3 | 52.03% | 4.71 | 2.95 | 0.485
NaNO3 | 95 | 2.257 g/cm3 | 36.59% | 4.60 | 2.69 | 0.418
NH4NO3 | 56 | 1.72 g/cm3 | 47.06% | 5.37 | 2.56 | 0.458
Icing sugar | 49 | 0.65 g/cm3 | 84.27% | 1.90 | 1.76 | 0.820
NH4NO3 & KNO3 Mixture | 68 | 1.94 g/cm3 | 38.89% | 4.63 | 2.41 | 0.472

## Slide 4
0%
100%
90%
20%
30%
80%
70%
60%
50%
40%
Mixture of icing sugar and NaCl
In volume fraction
Optical image
Microwave image

## Slide 5
Sugar Volume fraction(%) | Sample mass(mg) |  | -(MHz)
0 | 101 | 2.93 | 0.450
20 | 83 | 2.57 | 0.475
30 | 78 | 2.46 | 0.763
40 | 87 | 2.61 | 0.393
50 | 73 | 2.33 | 0.560
60 | 66 | 2.19 | 0.567
70 | 63 | 2.11 | 0.616
80 | 62 | 2.06 | 0.659
90 | 62 | 2.02 | 0.794
100 | 49 | 1.76 | 0.364
Sugar Volume fraction(%) | Sample mass(mg) |  | 
0 | 101 | 2.93 | 0.450
20 | 83 | 2.57 | 0.475
30 | 78 | 2.46 | 0.763
40 | 87 | 2.61 | 0.393
50 | 73 | 2.33 | 0.560
60 | 66 | 2.19 | 0.567
70 | 63 | 2.11 | 0.616
80 | 62 | 2.06 | 0.659
90 | 62 | 2.02 | 0.794
100 | 49 | 1.76 | 0.364

## Slide 6
Sensor design:
Penetration depth: ↑
Resolution: ↓
Penetration depth: ↓
Resolution: ↑
Resolution: ~ nm
Only surface properties
Summary:
    The resonant shift of the is approximate a linear relation as effective permittivity.
    It is unlikely to give the precise value due to large error bars.
    The spatial distribution of chemical powders can be obtained using this method.
Next step:
  Prepare more mixtures (two or three) and measure using of scanning technology.
  Determine the dielectric constant of chemical solutions using broadband technique.
    (non-resonant method).
  Compare these results with different methods.

## Slide 7
Finished first draft of the paper of dielectric imaging

## Slide 8
Signal:
By adding a extra dimension to the currently we have:
Assumption:
Theoretical prediction:
Discussion:
The active SSR is able to detect dielectric constant of different materials.
As for chemicals, it is influenced by the size of the chemical granules and surface inhomogeneity.
It is very difficult to distinguish explosive chemicals and normal materials by using this method.
Surface
Surface
Good result/ small error
Ok result/ large error
Plot in a.u.