## Slide 1: Determine Dielectric Constant in 1D Microwave Cavity
Yutong Zhao
Jan 15th ,2018

## Slide 2: Target
Determine the complex dielectric constant of different mediums:
  NaCl, NH4NO3, KNO3, NaNO3, KClO3 (humidity 0-10%)
  Mixture of two above (humidity 0-10%)
  Al powder
  Water
  Icing sugar (humidity 0-10%)
  Gasoline and diesel
According to DRDC’s contract section 6.5

## Slide 3: Resonance method
Frequency shift in 1D cavity:
  By writing down transmission matrix:
  Different sample will influence the matrix 


## Slide 4: Experiment setup

## Slide 5: Pure materials
Icing sugar sample
NaNO3 sample
1.57mm
Teflon
248mg
icing sugar
459mg
KClO3
494mg
NaCl

## Slide 6: Spectra vs. humidity
459mg KClO3
248mg icing sugar
309mg NH4NO3

## Slide 7: complex εr vs. humidity
Real part
Imaginary part

## Slide 8: Mixture: NH4NO3 in sugar(dry)

## Slide 9: Progress (~ 80%)
Material | Data collection | Data analysis
NaCl | √ | √
NH4NO3 | √ | √
KNO3 | √ | √
NaNO3 | √ | √
KClO3 | √ | √
Mixture: icing sugar & NH4NO3 | √ | √
Mixture: KClO3 & NH4NO3 | In progress(40%) | ---
Icing sugar | √ | √
Al powder | √ | √
Gasoline | √ | In progress
Diesel | √ | In progress
water | √ | In progress

## Slide 10: Aluminum powder and water
Water sample
Al powder sample

## Slide 11: Compare with Yao’s previous work
 |  | Yao | This work
Teflon |  | 2.06 | 2.114
KNO3 | powder | 3.7 | 
 | granule | 4 | 3.9106
NaNO3 | powder | 4.4 | 
 | granule | 4.5 | 4.6045
NH4NO3 | powder | 5.1 | 5.3663
 | granule | 4.9 | 
 |  | Recommended | 
Icing sugar |  | 1.5-2.2 | 1.8965