## Slide 1: Dielectric Constant Experiments Summary
Yutong Zhao
Jan 25th ,2018

## Slide 2: Task list
6.5.1 NaCl, NH4NO3, KNO3, NaNO3,KClO3 varying humidity from 0-10%
6.5.2 Mixing two powders of varying humidity from 0-10%
6.5.3 Aluminum powder
6.5.4 Water
6.5.5 Icing sugar (powder) humidity from 0-10%
6.5.6 Fuel oil (car gasoline and diesel)

## Slide 3: Experiment setup
Notes: 1 VNA connect the 1D cavity
2.Rotating angle was set as 45

## Slide 4: Simulations (E field, θ = 45o)
E-mode
H-mode
Z = 0 plane
S21
Notes: The simulation only show the result of E field at 45o.
For E-mode, the E-field reaches the maximum at center, and for H-mode, it reaches the minimum at center.

## Slide 5: Resonant method
1.57mm
Teflon
248mg
icing sugar
459mg
KClO3
494mg
NaCl
Error bar
1.09%
1.43%
0.97%
0.89%
0.96%
0.51%
0.38%
Sample | 
NaCl | 4.71
NH4NO3 | 5.37
KNO3 | 3.91
KClO3 | 4.36
Sugar | 1.90
NaNO3 | 4.60
Teflon | 2.11
Sample | 
NaCl | 4.71
NH4NO3 | 5.37
KNO3 | 3.91
KClO3 | 4.36
Sugar | 1.90
NaNO3 | 4.60
Teflon | 2.11

## Slide 6: Spectra vs. humidity
459mg KClO3
248mg icing sugar
309mg NH4NO3

## Slide 7: Empirical model for water content
-- dielectric constant at dry material
-- dielectric constant of water (57.95 + 32.72i) [Barthel et al];
a, b -- empirical parameter
-- conductivity loss parameter
-- water content in mass(%)

## Slide 8: Pure chemicals at humidity from 0-10%
Solid lines: calculation results
Real part
Imaginary
part
 | [Barthel et al] |  |  |  |  |  | 
Sample | a | b | Alpha | Sample | a | b | Alpha
KNO3 | 1.216 | 0.01 | 133.0 | NaCl | 1.104 | 0 | 315.5
NaNO3 | 1.208 | 0.7 | 28.5 | KClO3 | 1.152 | 0 | 40.7
NH4NO3 | 1.856 | 0 | 1650.5 | sugar | 0.216 | 0 | 8.4
Sample | a | b | Alpha | Sample | a | b | Alpha
KNO3 | 1.216 | 0.01 | 133.0 | NaCl | 1.104 | 0 | 315.5
NaNO3 | 1.208 | 0.7 | 28.5 | KClO3 | 1.152 | 0 | 40.7
NH4NO3 | 1.856 | 0 | 1650.5 | sugar | 0.216 | 0 | 8.4

## Slide 9: Mixture: NH4NO3 in sugar
Percent(%) | a | b | Alpha
0 | 0.216 | 0 | 8.4
20 | 0.522 | 0 | 80.5
40 | 0.656 | 0 | 109.5
50 | 0.536 | 0 | 57.5
60 | 1.176 | 0.4 | 84.5
75.87 | 1.624 | 0.4 | 144
100 | 1.856 | 0 | 1650.5
Imaginary part
Real part

## Slide 10: Task list
6.5.1 NaCl, NH4NO3, KNO3, NaNO3,KClO3 varying humidity from 0-10%
6.5.2 Mixing two powders of varying humidity from 0-10%
6.5.3 Aluminum powder
6.5.4 Water
6.5.5 Icing sugar (powder) humidity from 0-10%
6.5.6 Fuel oil (car gasoline and diesel)

## Slide 11: Problem: water and Al powder
= 3.7%
= 7.9%
water

## Slide 12: Non-resonant measurement (theta = 0o)
Sample
Air
Air
Port 1
Port 2
Surface 1
Surface 2
L
R
 Measure 4 S parameters
Define transfer matrix
Fit result

## Slide 13: Definition of transfer matrix
Sample
Air
Air
Surface 1
Surface 2
L
R
Standard measure
Sample measure
Tran
Refl
I
surface
Tran

## Slide 14: Raw data and fitting results

## Slide 15: Car fuel Measurement
=3.016+0.196i
= 2.666 + 0.028i

## Slide 16: Task list
6.5.1 NaCl, NH4NO3, KNO3, NaNO3,KClO3 varying humidity from 0-10%
6.5.2 Mixing two powders of varying humidity from 0-10%
6.5.3 Aluminum powder
6.5.4 Water
6.5.5 Icing sugar (powder) humidity from 0-10%
6.5.6 Fuel oil (car gasoline and diesel)

## Slide 17: Next step
Redo measurement of water.

## Slide 18
35-40
50-60