## Slide 1: Data analysis & Empirical Model of dielectric constant measurements
Yutong Zhao
Jan 22nd ,2018

## Slide 2: Determined gasoline and diesel
=3.016+0.196i
= 2.666 + 0.028i
Gasoline absorb microwave at dry!
Notes: We found that gas have a significate large imaginary part epsilon. Also that of diesel is not negligible.

## Slide 3: Problems of Al and water
Other paper
=57.95 + 32.72i
[Barthel et al]
Our result
=48.06 + 38.63i
Our result
= 199.65 + 0.957i
Similar result:
ceramic-powder polymer
[Bai, Y., et al(2000)]
H mode
Notes: These results are doubtable because the resonate peaks are so close to H mdoe , we are planning doing these measurement in a different method.

## Slide 4: Empirical Model for Soils
: Wilting points (plants concept)
P : Porosity of dry soil
Dielectric constant for air, water, rock and ice
: Fitting parameter
with
If
Wang, J. R., & Schmugge, T. J. (1980).
IEEE Transactions on Geoscience and Remote Sensing,
(4), 288-295.
Notes: I have found a dielectric model for different soils, it is an empirical model with a lot of parameters.

## Slide 5
Real part
Imaginary part
Different soil at 5 GHz
Data and model fit at 5 GHz
Notes: Based on their paper, their model agrees with measurement quite well.

## Slide 6: Simplified model
No air , P = 0 and no ice involved
Replace (rock) with (dry)
Consider conductivity loss
Next step fitting

## Slide 7: Fitting results at = 0
KClO3
Sugar
NaCl
NaNO3
KNO3
NH4NO3

## Slide 8: Method for water & Al powder
Transmission /Reflection(T/R) method
Sample
Air
Air
Port 1
Port 2
Transmission Matrices

## Slide 9: Eliminate systematic error x & y
Standard :
Sample :
Many complex value of can satisfy the function
Need a good initial guess!
Data collection completed

## Slide 10: Next step
Analysis data by setting ≠ 0 in empirical model for water content.
Build a Matlab code calculate the using T/R method.