## Slide 1: Complex permittivity of water at room temperature
Jan 14th 2019
Yutong Zhao

## Slide 2
Re
Im
1.40mm RO-5880 material
The shift may caused by the existence of TM01 mode
Cutoff frequencies
Resonant method: Yao’s 1D cavity
Non-Resonant method: rectangular waveguide
1.34mm RO-5880 material
More noisy and not accurate than resonant method
Empty
RO5880
Empty
RO-5880

## Slide 3
Measured Temperature
Purity of the de-ionized water:
Debye model of water
at different temperatures
Debye model of water
according to our lab

## Slide 4
Debye model of water at
and measured data of water
Resonant method
Water problem:
Due to the large absorption, the shifted peak is hard to find.
This method is inaccurate for large material.
Non-Resonant method
Broadband measurement can determine the dielectric constant of water.

## Slide 5
X band: 1.450 mL and 1.153 mL
Ku band: 0.485 mL and 0.982 mL
8 – 12GHz
12 – 18GHz
Debye relaxation for water [1]:
, , , , --- fitting parameters
[1]
(Fixed)
(Fixed)
ps
ps (Fixed)
Fitting results
Re
Im
Fixed at

## Slide 6
Debye relaxation model for water solutions[2]:
--- dc conductivity
--- vacuum permittivity (F/m)
[2]